## PRODUCT SPECIFICATION

Product Type - Metal Free, 5mm, Close Mesh Hairnet

Product Reference	Hair-TEC® 843K

Product Description	5mm Close Mesh Hairnet with our industry leading lay flat, double elastic headband to distribute pressure evenly  and avoid skin indentation and discomfort.

Closure	Welded, Metal Free – lays flat to avoid discomfort

Structure	Warp knitted, 5mm diamond mesh, double elastic headband

Composition			94.8%  Polypropylene, 5.2% Latex.

Manufactured from Polypropylene for excellent moisture transportation and wicking properties.  Additionally, our Latex is covered with polypropylene to avoid skin allergy and discomfort.

Size			21" [53cm] closure to closure - tolerance + / - 1"[2.5cm]

Weight GSM		11gsm+-5%

Weight per unit		1.81g+-5%

Colourfastness to Rubbing		BS EN ISO 105-X12 – 5/5

Colourfastness to Perspiration	BS EN ISO 105 – 4/5

Mesh Flame Retardancy 		BS EN ISO 1021-1/2:2006 - Pass

Colour Availability			Blue, White, Red, Green, Yellow, Black, Brown,  Blonde, Pink

Presentation			50 nets on round card

100 nets (2 round cards) per unit pack

or

50 nets in dispenser pack

or

100 balled nets in grip top bag

or

144 nets (3 round cards of 48) per unit pack

Pack free from elastic band

Notes:  This product falls outside of the “materials in contact with food” regulations.  The product’s sole intention is to protect the food from contamination by the wearer – hence the product and food are not in contact with each other.

Please note that  these yarns are hypoallergenic but care should be taken with wearers who express a sensitivity to latex.